## Slide 1: Industrial chemistry
Kazem.R.Abdollah
Rubber

## Slide 2
The word “rubber” immediately brings to mind materials that are highly flexible and will snap back to their original shape after being stretched.
The term “rubber” was coined for this material by the English chemist Joseph Priestley, who noted that it was effective for removing pencil marks from paper.
Rubber products appear everywhere in modern society from tires to biomedical products.

## Slide 3
The worldwide demand for rubber was estimated to be 23.0 million metric tons for 2011, excluding latex materials.
Of this demand, 36% is synthetic rubber of various kinds.
The major general purpose rubbers are natural rubber, styrene–butadiene rubber (SBR), butadiene rubber, isoprene rubber, and ethylene–propylene rubber.
These rubbers are used in tires, mechanical goods, and similar applications.
SBR, butadiene rubber, and ethylene–propylene rubber account for 78% of all synthetic rubber consumed.

## Slide 4: Rubber Concepts
1. Polymer structure:
a) Macrostructure
Molecular weight
Molecular weight distribution
Branching
b) Microstructure
c) Network structure
2. Rubber properties:
a) Elasticity—the retractive force
b) Glass transition temperature
c) Crystallinity
3. Rubber use:
a) Compounding
b) Processing

## Slide 5: a) Macrostructure
Molecular weight :
The single most important property of any polymer is the size or length of the molecule.
Most of the monomers used to produce rubbers are either gases or low-viscosity liquids under normal conditions; upon polymerization they form liquids whose viscosity increases to extremely high values as the chain length is increased.
In addition to viscosity, a great many other physical properties of any polymer depend upon the molecular weight.

## Slide 6: a) Macrostructure
Molecular weight distribution:
A given polymer sample is composed of many polymer chains, which in most cases are not of the same length.
For economic reasons, it is not possible to separate the various polymer chains by length prior to use.

## Slide 7: a) Macrostructure
Branching:
The concept of a polymer chain implies two ends per chain.
However, because of the nature of the process used to form the polymer, the chain may contain one or more branch points, resulting in multiple ends per chain. These chain ends can have an adverse effect on polymer performance.

## Slide 8: b) Microstructure
In the formation of elastomers from diolefin monomers such as butadiene or isoprene, there are a number of possible structures. The possible polyisoprene structures are:
For butadiene (no methyl group) the 3,4 form does not exist.
The 1,2 addition is referred to as vinyl addition.

## Slide 9: c) Network Structure
For most rubber systems the network is formed after the polymer is compounded and molded into the desired final shape.
Once cross-linked, the material no longer can be processed. If cross-linking occurs prior to compounding or molding, the material is referred to as gelled, and it cannot be used.

## Slide 10: 2. Rubber Properties
    Elasticity: The Retractive Force:
    The important, and most interesting, result of these theories is that rubber elasticity arises from changes in entropy of the network.
    Rubber molecules are capable of geometric isomerization, examples of which are cis and trans, just like any other unsaturated organic molecule. Upon stretching the network of chains, no “configurational” changes take place. That is, cis is not changed to trans and thus there is no configurational contribution to entropy.
    Elasticity does not arise from stretching or deforming covalent bonds either.

## Slide 11
The chains do not like being in a stretched state because there are many conformational states not available to them until the stress is released.
The following expression, for extensions >10%, shows that the elastic force, f, is directly proportional to the absolute temperature, or the elastic response of the rubber is entirely governed by the decrease in entropy (S) which it undergoes upon extension. The term ∂L is the change in length of the sample:
for constant temperature and volume

## Slide 12
The shear modulus of the rubber network is related to the molecular weight between cross-link points or Mc. The lower the molecular weight of chains between cross-links (network chains), the higher the cross-link density and the higher the modulus. This is shown in the following expression:
where G0 is the elastic shear modulus, is the density, R is the gas constant, and T is absolute temperature.

## Slide 13: b) Glass Transition Temperature
As the temperature is lowered, the ability of the chain segments to move decreases until a temperature is reached where any large-scale motion is prevented. This temperature is referred to as the glass transition temperature (Tg).
Below this temperature the rubber becomes a glassy material—hard and brittle.
Above this temperature amorphous plastics, such as polystyrene, can exhibit a rubbery character if the molecular weight is sufficiently high.

## Slide 14: c) Crystallinity
The existence of strong interchain interactions via polar forces, hydrogen bonding, or ionic groups can facilitate crystallization.
Rubbery materials must have both their melting temperature (if they have a crystalline point) and their glass transition temperature below the use temperature.

## Slide 15: 3. Rubber Use
  Compounding:
  The rubber industry began when Charles Goodyear developed the first useful rubber compound: natural rubber plus sulfur.
  The major components in a compound are
  curatives
  reinforcing agents
  fillers
  plasticizers
  and antidegradants

## Slide 16: Curatives
The function of curatives is to cross-link the polymer chains into a network; the most common ones are the sulfur type for unsaturated rubber and peroxides for saturated polymers.
Chemicals called accelerators may be added to control the cure rate in the sulfur system; these materials generally are complex organic chemicals containing sulfur and nitrogen atoms.

## Slide 17: Reinforcing agents
Carbon black and silica are the most common reinforcing agents.
These materials improve properties such as tensile strength and tear strength; also, they increase hardness, stiffness, and density and reduce cost.
In tire applications, new polymers are currently being developed which contain functional groups that directly interact with carbon black and silica, improving many properties.

## Slide 18: Fillers
Fillers are added to reduce cost, increase hardness, and color the compound.
Generally they do not provide the dramatic improvement in properties seen with reinforcing agents, but they may have some reinforcing capability.
Typical fillers are clays, calcium carbonate, and titanium dioxide.

## Slide 19: Plasticizers
These materials are added to reduce the hardness of the compound and can reduce the viscosity of the uncured compound to facilitate processes such as mixing and extruding.
The most common materials are petroleum based oils, esters, and fatty acids.

## Slide 20: Antidegradents
This group of chemicals is added to prevent undesirable chemical reactions with the polymer network.
The most important are the antioxidants, which trap free radicals and prevent chain scission and cross-linking.
Antiozonants are added to prevent ozone attack on the rubber, which can lead to the formation and growth of cracks.

## Slide 21: 2. Processing
A wide range of processes are used to convert a bale of rubber into a rubber product such as a tire.
The first process generally will be compounding.
In many compounds more than one rubber may be needed to obtain the performance required.